## Slide 1
表面生长晶须对氧化铝陶瓷钎焊的影响规律研究
EFFECTS OF THE GROWN WHISKERS ON BRAZING OF ALUMINA
哈尔滨工业大学材料科学与工程学科
第十三届研究生模拟国际学术会议(2018)
材料加工工程学科12级***博士，***教授
***618667@126.com
研究背景/ Objective
主要创新成果/Innovative Results或研究思路/ Research ideas
Y.F. Wang, J.C. Feng, Z.C. Chen, X.G. Song, J. Cao. Wetting of microstructured alumina fabricated by epitaxial growth of Al4B2O9 whiskers. Applied surface science, 2015, 357: 766-770.(1f=X)
Y.F. Wang, J. Cao, Z.J. Wang, Z. Chen, X.G. Song and J.C. Feng. Temperature-dependent transformation from whisker- to nanoparticle-strengthened composite interface in the Al2O3/Ag-based alloy system and mechanical properties of the joints. Materials Characterization, 2015, 109: 50-56. (1f=X)
Y.F. Wang, J.C. Feng, Z.J. Wang, X.G. Song and J. Cao. Joining of Al2O3 via the epitaxial growth of aluminum borate whiskers for high-temperature applications. Materias Letters, 2016, 163: 231-235. (1f=X)
代表性文章/Publications
Fig.1 Characterization of the grown whickers
Al2O3 is widely used in numerous areas due to its ultra-high melting temperature, excellent oxidation resistance, and high strength. Fabrication of topographically altered surfaces is beneficial to wetting on alumina and increasing the quality of alumina brazing joints.
Fig.2 Wetting curves on alumina
Fig.3 Microstructure of the whisker-coated Al2O3 joints
1. Topographical microstructures were fabricated on alumina by epitaxial growth of Al4B2O9 whiskers in air.（Fig.1）
2. The time needed to reach the equilibrium wetting stage reduced as the temperature increased, and the final contact angle for liquid Ag-36.7Cu-8.0Ti at.% alloy on the rough surface was 27° at 880 ℃.（Fig.2）
3. As the bonding temperature increased, the Al2O3/AgCuTi interface was found to transform from whisker- to nanoparticle-strengthened composite region.（Fig.3）
4. Both whiskers grown on Al2O3 and the dispersive nanoscale products in the alloy played positive roles in improving the joint properties. （Fig.4）
Fig.4 Effect of whiskers on bend strength of Al2O3 joints